## Slide 1
Application of ZINGA Film Galvanising On Railway Transport
www.zinga.eu www.zinga.cn

## Slide 2: Primo Corporation (Shanghai) Ltd. ZINGA Film Galvanising - Exclusive Distributor China

## Slide 3: ISO 12944 – Standard for steel structure corrosion protection ISO 12944 is currently the most authoritative international standard for corrosion protection of steel structure coatings. It sets the guidelines and norms for formulating corrosion protection schemes of steel structures.

## Slide 4: 1、ISO 12944-2: Atmospheric Corrosive Environment Classification Environmental rating is based on the weight of carbon steel lost within one year of exposure to different environmental conditions
Classification of environments | Corrosion level | Mass loss (g/m²) | Typical outdoor environment | Typical indoor environment
C1 | Very Low | <10 | Rural / dry areas, neutral atmosphere | Heating room
C2 | Low | 10～200 | Low pollution, dry area | Condensation may occur in unheated rooms
C3 | Medium | 200～400 | Urban and industrial atmosphere, moderate SO2 pollution | High humidity, some places polluted by air
C4 | High | 400～650 | Industrial and coastal environment | Chemical plant, swimming pool
C5 – I C5 –M | Very high (Industrial) M Very high (Marine) | 650～1500 | Coastal and offshore buildings | Buildings and places where there is always condensation and high humidity
CX | Extremely severe corrosion | 1500～5500 | High salinity in coastal and offshore areas and harsh industrial areas | Buildings and places that are always in high humidity and heavy pollution

## Slide 5: ● For different coating systems, the Standard specifies the anticorrosive life of the coating under different environments, and it is classified into three ranges: short-term (2-5 years), medium-term (5-15 years) and long-term (> 15 years). ● The definition of anti-corrosion life is similar to the design life in engineering design, that is, the life of the first overhaul of the coating system .
2、ISO 12944-5: Specification of
of anticorrosive life

## Slide 6
Corrosion of steel
Cathodic protection
Non-cathodic protection
Coating system
Coating system
Protective coating
generates
Reacts to air and moisture
Corrosion occurs
No corrosion
Fe
Fe
zinc
zinc
paint
paint

## Slide 7
Barrier protection
Single coating
Multi-layer coating
Additional material
Cathodic protection
Electrophoresis / electroplating
Hot dip galvanizing（HDG)
Thermal spray zinc / aluminum (by torch or electric arc)
Cold applied film galvanized
Common commons of industrial corrosion protection

## Slide 8
Product name | Packing
Zinga | 1、2、5、10、25 Kg/can
Zingasolv | 1、5、25 L/can
Aquazinga | 10、25 Kg/set
Zingaspray | 500 ml/can
Packing Specifications

## Slide 9
Current Activities
Production and sales of ZINGA range
of products
Expansion of distributorship
95 distributors in >100 countries:
  Africa, Asia, Australia & NZ
  Europe, Middle East
  North & South-America
Expansion of range of products
  ZINGA as primer or shop-primer
  ZINGA as stand-alone system
  Sealers
  Topcoats

## Slide 10
ZINGA
1. Zinc powder - refined by
atomization
ɸ 3－5 μm
Zinc content in dry film = 96％
Zinc powder purity = 99.995%
(no lead, cadmium or other heavy metals）
2. Neutral resin: conductive
3. Aromatic solvent: naphtha; non-
toxic
Zinc Rich Paints
1. Zinc powder - refined
by distillation
ɸ 12－15 μm
Zinc content in dry film = 70-85％
Zinc powder purity = 98％
(contains heavy metals such as
lead & cadmium ）
2. Organic resin
3. Solvent contains harmful toluene,
xylene, acetone
Comparison of ZINGA
and Zinc Rich Paints

## Slide 11
Advantages of ZINGA
Durable Corrosion Resistance
1. Determination of resistance to neutral salt spray ：9500 hours
2. Corrosion rate 1/3 of hot-dip（corrosion rate as immersed in salt solution ）
HDG = 0.110 mm/yr
ZINGA = 0.035 mm/yr
3. ISO 12944-6 certifications
- ZINGA 2 x 60 µm
- ZINGA 2 x 90 µm
- ZINGA 60-80 µm + epoxy MIO intermediate paint 120 µm
+ finish 60 µm [C5-I High]

## Slide 12
Advantages of ZINGA
Coating Characteristics
Good adhesion - test results：0-1 (cross-cut method)
6.5–10.1 Mpa (pull-off method)
2. Excellent flexibility (Φ1 mm) & impact resistance (50 mm)
3. Excellent abrasion resistance：0.0451 g (500g,1000 revolutions)
4. Excellent moisture and heat resistance; wide working
temperature range：-40℃～150℃
5. Weldability - DFT <60 µm not affecting welding quality
6. Unique reliquidability, repeated overcoating without having to remove old layers

## Slide 13
Advantages of ZINGA
Application Performance
ZINGA is single component, easy to apply and repair /maintain.
Can be applied by air support /airless spraying, brush, roller, dipping, electrostatic spraying.
Surface treatment not demanding, and can be applied on rusted surface (St 2).
Dries quickly – touch dry in 10-15 minutes (below 23 C)
5. Can be applied on wet metal surfaces
6. Can be applied under ambient condition of relative humidity ≤ 95%

## Slide 14
Advantages of ZINGA
Product Performance
Active, cathodic, galvanic
protection → very high zinc
content (96%)
vs hot-dip, metallisation
  Passive barrier protection
  → zinc salts on top of surface
  vs protective paints
One component organic zinc coating
ZINGA is NOT a paint
- Does not form a closed film
- Will never crack
- will never peel off
Untreated
Treated except 2cm strip
ZINGA layer

## Slide 15
Advantages of ZINGA
Product Performance
Galvanised structures can be recharged or reloaded with ZINGA
ZINGA on ZINGA
ZINGA on metallised or HDG
Each new layer of ZINGA blends perfectly with the previous one
Additional layers all blend to form one single, homogeneous ZINGA layer
Copper particles on top of ZINGA
Application of 2nd pass ZINGA on copper particles ;
The copper particles blend
in the two layers of ZINGA
Copper particles in between
the two layers of epoxy paint.
Epoxy does not blend together !

## Slide 16: ZINGA Anti-corrosion Principle

## Slide 17
ZINGA vs Zinc Rich Paint
ZINGA
Zinc rich paint
ZRC zinc particles are 3--5 times larger than Zinga zinc particles

## Slide 18
ZINGA vs Zinc Rich Paint

## Slide 19
Electrode potential measurement
ISO 15711-2003
Electrode potential measurement
Determination of coating sacrificial anode and protective cathode performance ：
ZINGA = -1114 mV
Zn rich paint = -752 mV
Uncoated = -682 mV
Other zinc rich paint
ZINGA
ZINGA vs Zinc Rich Paint

## Slide 20
After 7 days of exposure to salt water
Immersion test
ZINGA vs Zinc rich paint
Other zinc rich paint
ZINGA

## Slide 21
Project References

## Slide 22
Project ： Shanghai Maglev TransRapid – functional parts
Location ：Shanghai (Lujiazui to Pudong Int’l Airport, 37 km)
Cating system ：ZINGA 80 µm + Epoxy sealer 30 µm + Epoxy micaceous iron intermediate paint 100 µm + Over-coatable polyurethane finish 60 µm

## Slide 27
Project ： Zuibaichi Station of Shanghai Metro Line 9
Location ：Shanghai
Coating system ：ZINGA 60 µm + Epoxy sealer 30 µm + Epoxy micaceous iron intermediate paint 100 µm + Fluorocarbon finish 60 µm

## Slide 29
Project ：Chongqing Monorail Line 1
Location ：Chongqing
Coating system ： ZINGA stand-alone on rebars 1 x 40 µm；
PC column support plates 2 x 50 µm
Completion date ：2001.7.30

## Slide 32
Project ： Chongqing Monorail Line 1 Track Bifurcation
Location ：Chongqing
Coating system ：ZINGA 60 μm + Epoxy sealer 30 μm + Epoxy micaceous iron intermediate paint 80 μm + Over-coatable polyurethane finish 2 x 30μm
Completion date：2001.7.3

## Slide 34
Project ：Beijing-Shanghai High-speed Railway Link
(protection of rebars)
Location ：Xuzhou to Tangshan section
Coating system ：ZINGA stand-alone 1 x 40 μm

## Slide 36
Project ： Shanghai Metro Line 11
Location ： Shanghai
Coating system ：ZINGA stand-alone 2 x 60 m

## Slide 38
Project ： Shenzhen Metro Line 1
Location ：Shenzhen
Coating system ：ZINGA stand-alone 2 x 60 m

## Slide 40
Project ： Beijing Metro Line 4
Location ： Beijing
Coating system ：ZINGA stand alone 2 x 60 µm

## Slide 42
Project ： Beijing Intercity Railway S2 Line
Location ： Beijing
Coating system ：ZINGA stand-alone 2 x 60 m

## Slide 44
Project ： Guangzhou Metro Line 3
Location ： Guangzhou
Coating system ：ZINGA stand-alone 2 x 60 m

## Slide 46
Project ： Hong Kong MTR
Location ： Hong Kong
Coating system ：ZINGA stand-alone 2 x 60 m

## Slide 48
Project ： Guangzhou-Shenzhen-Hong Kong High-speed
Railway - Hong Kong section
Location ： Hong Kong
Coating systems ： Reinforcement of underground space at West Kowloon Terminus - ZINGA 1x 40 um；steel structures of terminal building - ZINGA 60um + Epoxy micaceous iron intermediate paint 120 um ＋ Polyurethane finish 50 um

## Slide 51
Project ： Guangdong Yuehai Passage Railway – pier steel
fenders
Locations ：Haikou, Hainan and Zhanjiang, Guangdong
Coating system ：ZINGA 2 x 40 μm + AUQAZINGA 2 x 40 μm
Completion date：Dec 2001

## Slide 54
Project ： SMRT
Location ：Singapore
Painting scheme ：ZINGA stand-alone 2 x 60 m

## Slide 57
Project ： London Underground
Location ： London
Painting scheme ：ZINGA stand-alone 2 x 60 µm

## Slide 59
涂装前

## Slide 60
Project ： Brasilia Railway
Location ： Brasilia, Brazil
Coating system ：ZINGA stand-alone 1 x 80 µm

## Slide 63
Project ： Onping 360 SkyRail Cable Cars
Location : Lantau, Hong Kong
Coating system : ZINGA stand-alone 2×75 μm
Completion date: 2006

## Slide 70
Project ： Guangzhou New TV Tower Ferris Wheel
Location ：Guangzhou
Coating system ：ZINGA 80µm＋Epoxy sealer 30µm＋
over-coatable polyurethane finish 60µm
Completion date: 2010.9